## Slide 1
Group 4 Keynote
Icorr Young Engineers Programme 2020
Glycol Desalination Plant Failure

## Slide 2
Change

## Slide 4
Condition State
Change
Strategies
Priorities
Systems & Processes
Individual skills
Visible Symptom

## Slide 5
Set out + be curious
Explore
Learn more
Focus + keep improving
Create
Challenge
Vision
Technical excellence
Executional excellence
Deliver
Go
Set Course
Final Approach
Get ready

## Slide 6
Ryan Cobbs
Civil Engineer
Praveena Nanthakumaran
Mechanical Engineer
Izabela Gajewska
Corrosion Engineer
Vincent Lemoine
Welding Engineer
Harry Wright
Corrosion Engineer
Tasos Kostrivas
Mentor

## Slide 7
Fusion
Degradation Mechanisms
Corrosion Risk Assessment
QA
Mitigation Options
Conclusion
Introduction
Group 4

## Slide 8: Background
Fusion
Group 4
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction
8

## Slide 9
Viscous (syrup-like), colourless and odourless alcohol
Oil & Gas: used as a gas-hydrate inhibitor to prevent the formation of gas hydrate during natural-gas production
Fusion
Group 4
PROs | CONs
Can recoup/recover - lower impact on environment and economic advantage | Toxicity to humans and animals
Reduce the risk of gas hydrate formation in pipelines* | Natural tendency to degrade in the presence of oxygen and heat*
Low viscosity – can run pumps at a lower speeds (less energy) | Effect of salt and its precipitation
…? | Acidic – accelerate corrosion, e.g. CS*
9
Mono-Ethylene Glycol / MEG / (CH₂OH)₂
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction

## Slide 10
What is it?
It is the removal of salts and minerals from a target substance
In context?
The removal of salts from MEG
But where is this coming from?
Recycling the MEG
The process of MEG recovery?
Fusion
Group 4
10
Desalination of MEG
Pre-Treatment
Desalination
Regeneration
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction

## Slide 11
Fusion
Group 4
11
Overall plant process
Fig 1: Basic overview of offshore gas process plant
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction

## Slide 12
Fusion
Group 4
12
Desalination plant
Fig 2: Desalination plant
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction
Leaks

## Slide 13
Fusion
Group 4
13
Process conditions
3-7 pH
Organic acids
~120°C
High operating conditions
<10ppb
Oxygen ingress
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction

## Slide 14
Fusion
Group 4
Commonly used in Oil & Gas as well as Chemical Industry (Desalination Plants)
Passive layer of durable oxides TiO2 forms a “shield” against oxygen and prevents corrosion
High resistance to corrosive species (eg Chlorides)
Grade 12 has significant resistance to crevice corrosion in hot brines compared to unalloyed Titanium
Titanium
O
Passive layer TiO2
O
Materials of Construction Titanium Grade 12
14
Fig 3: Passive layer formation
MEG
Desalination of MEG
Process description
Process conditions
Materials of Construction
Fig 4: Crevice corrosion guideline for titanium [3]
crevice corrosion is possible here
135 (max)

## Slide 15: Degradation Mechanisms
Fusion
Group 4
What happened?
Observed failures
Pitting / Crevice Corrosion
Hydrogen Embrittlement
Welding
15

## Slide 16: Degradation Mechanism Observed failures
Fusion
Group 4
Fig 5: Visual examination of sections from titanium spool: a) Close up of leaking area in recycle line spool (outer surface) b) Section of sample JA1 (inner surface)
Pits
Cracks
Fig 6: Crack in the weld observed in titanium spool section MetJB1
16

## Slide 17
Fusion
Group 4
Fig 7: Mono-ethylene glycol oxidation
Oxygen ingress
MEG degradation
Low pH
Pitting / Crevice corrosion
High temperature
Chlorides
Erosion
Fig 8: Spool sectioning. Blue lines shows the fluid path
Fig 9: Pit on the internal Titanium Grade 12 surface: a) spool section photograph b) spool section light metallograph
Salts deposits
17
b)
a)

## Slide 18
Fusion
Group 4
Fig 11: Effect of temperature and pH crevice corrosion of Titanium Grade 12 in saturated NaCl brine [3]
Fig 10: Crevice corrosion mechanism for titanium in aqueous chloride media [1]
crevice
anodic site
cathodic site
salt deposit
Pitting / Crevice Corrosion
Crevice corrosion, next to pitting, was one of the primary degradation mechanisms
Pits developed on the salt-free surface and crevices developed under the slurry salt deposits
Because of the small, restricted volumes of solution within tight crevices pH levels as low as 0 to 1 can develop
18
135℃

## Slide 19
Fusion
Group 4
Metal oxidation
Ti Ti 4+ + 4e-
Hydrogen Evolution
Oxygen Reduction
O2 + 4H+ + 4e- 2H2O
4H+ + 4e- 2H2(g)↑
Hydrogen present in the fluid originated from the primary corrosion reaction.
Fig 12: Corrosion mechanism for titanium
Metal oxidation
Ti Ti 4+ + 4e-
Hydrogen Evolution
Oxygen Reduction
4H+ + 4e- 2H2(g)↑
O2 + 4H+ + 4e- 2H2O
Pitting / Crevice Corrosion
19

## Slide 20
Fusion
Group 4
H2 from Pitting / Crevice Corrosion
Hydrogen Embrittlement / HIC
Sensitive location - HAZ
Fig 13: SEM backscattered image of the fracture face showing internal fracture plans (cleavage-like brittle fracture)
The brittle fracture occurred due to:
  Hydrogen absorption
  Sensitive location at the weld i.e. HAZ
  Microstructure susceptible to cracking
Microstructure
Fig 14: SEM backscattered image of fracture face near outside surface (ductile fracture)
Hydrogen Embrittlement
Hydrogen Embrittlement and Hydrogen-induced Cracking (HIC) were the most credible secondary degradation mechanisms
20
Fig 15: The crack and the fracture face in section MetJB1
Titanium
hydride layer
Ligament
(Titanium Grade 12)

## Slide 21
Fusion
Group 4
Hydrogen was channelled towards the Titanium Grade 12 bulk along grain boundaries where β phase was concentrated (i.e. white lines in the Figure X. b)
β phase is known to be an easy path for hydrogen transport as it has relatively “loosely” packed structure and hence, higher diffusivity and solubility of hydrogen than α phase
Hydrides precipitated in the closed-pack α phase as it has limited space to dissolve hydrogen
intergranular crack
β phase
α phase
Fig 16: SEM backscattered images: a) cleavage cracking b) intergranular crack
a)
b)
Hydrogen Embrittlement
21
Note: Hydrides dissolve easily in temperature above 100 to 150°C allowing hydrogen diffusion within the material [10]. Max temperature in MEG system was 135°C.

## Slide 22
Fusion
Group 4
Coarse structure in HAZ
Brittle structure
Critical location for Hydrogen Embrittlement
Welding Coarse structure in HAZ
22
Fig 17: HAZ Micrograph
Fig 18: BM Micrograph

## Slide 23
Fusion
Group 4
Intersection HAZ longitudinal and branch welds
β phase
α phase
Welding Titanium Sensitization
23
Figure 19: Failure location
Figure 20: Titanium phases and Ti2Ni
Thermal history at failure location
Precipitation Ti2Ni intermetallic at
α/β phase boundaries
Grain boundaries weakened by
Ni depletion
Preferential corrosion sites

## Slide 24: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Outcome & final risk level
Acceptable
risk?
What are the mitigation options?
24

## Slide 25: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Outcome & final risk level
Acceptable
risk?
What are the mitigation options?
Loss of containment
Volume
Toxicity
Temperature
Dynamic Pressure
Flammability
Injury to operators
Single use MEG
Financial losses
70
p/week
Increased Pollution
Temporary outage
25

## Slide 26: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Outcome & final risk level
Acceptable
risk?
What are the mitigation options?
Total disruption
corrosive environment
material selection
engineering application
Failure mode:
Loss of containment
Corrosion damage:
Crevice corrosion
Pitting corrosion
Cracking
Output concerns:
Thermal degradation of MEG in presence of oxygen which leads to accumulation of organic acids imposing corrosion mechanisms which could result in dissolution and embrittlement of metal.
Controlled by oxygen levels below 10ppb
requires strengthening
corrosion damage
requires maintenance
26

## Slide 27: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Outcome & final risk level
Acceptable
risk?
What are the mitigation options?
Consequence
Probability
×
Risk Level
=
5/5
4/5
20
(high risk)
Probability
Consequence
1
2
3
4
5
1
2
3
4
5
low risk
medium risk
medium - high risk
high risk
Probability | Low chance of occurrence……....almost certain to occur
Consequence | Not serious……………………. total failure safety hazard
Ranking Value | 1 2 3 4 5
27

## Slide 28: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Acceptable
risk?
What are the mitigation options?
Eliminate
Control
Reduce
Isolate
Material Selection
Chemical treatments
Coatings
Process & environmental control
Principles
Outcome & final risk level
28

## Slide 29: Risk Assessment
What are the hazards
What are the consequences?
What is the probability?
Corresponding risk level
Outcome & final risk level
Acceptable
risk?
What are the mitigation options?
Environmental Control
De-stable the corrosion processes
Emergency Repairs
Procedures in place to undertake effective and fast repairs
Long-term Solutions
Plan long-term to reduce maintenance requirements
Risk Management
Mitigation Options
Effective Inspections
Identify damages and repairs early before they lead to disruption
29

## Slide 30: Mitigation Options
Fusion
Group 4
Environmental Control
Effective Inspections & Management
Temporary Spool Replacement
30

## Slide 31
Mitigation Options
31
Fusion
Group 4
Environmental Control
What factors effect the corrosion process?
Can they be managed?
Variable | Process condition | Action | Why? | Feasibility
Temperature | 120oC | Reduce temperature to <110oC | Prevent thermal degradation of MEG in presence of oxygen | Regeneration of MEG requires temperatures >120oC
pH | 6-7 | Stabilise pH | Reduce hydrogen ions available for cathodic reaction | CAPEX/OPEX Scale formation
Oxygen levels | <10ppb | Staff training Reinforce seals Increase N2 blanket purity | Minimise oxygen intrusion | Feasible

## Slide 32
Goal 1 identify damages
Goal 2 identify repairs
Goal 3 identify critical areas
Goal 4 establish control points
Mitigation Options
32
Fusion
Group 4
Effective Inspections &
Management
Are there areas of concern?
Specialist
Investigation
Measure Performance by Monitoring
Input data
During outage with borescope
Areas of concern need further investigation such as radiography
Repeat process and make changes where necessary
Proactive monitoring using same external examination techniques
Meeting control criteria?
Scope
Basic Inspection: External examination & thermography to identify leaks in operation
Specialist inspection: Likely to comprise radiography techniques
Internal / External Examination
Establish Control Criteria
Yes
No
No
Yes
Thermography to identify leaks under insulation
increase number of effective inspections = increase confidence of the outcome
Escalate emergency repair procedure
?
No
Yes

## Slide 33
Group 4
Under monitoring of the stream corrosivity
Grade X52 was selected
Connection by standard flanges (ASME B16)
Rubber gasket between flanges
Ceramic coated bolts & washers
ASME B31-3 section 304.1.2:
(Corrosion rate 1.67mm / year + oxygen level 100ppb + temperature 128⁰C)
(Standard NPS thickness for 1” tubes)
Standard flanges ASME B16
Figure 22. Corrosion rates for carbon steel – Additional information ICorr
Mitigation Options Emergency Repairs
33
Fusion
Figure 21: Spool flanges

## Slide 34
Properties | Carbon Steel | Stainless Steel | Nickel-based Alloys | Titanium
Erosion resistance | Low | Relatively good | Relatively good | Excellent
Corrosion resistance in organic acids environment | Low (i.e. hydrogen cracking is possible in high strength carbon steel) | Depends on the steel grade (i.e. 300 series and duplex shows generally good resistance) | Relatively good | Good to excellent (even if the air or other oxidants are present)
Hydrogen Embrittlement susceptibility | Relatively low | High (generally increasing with alloy strength) | Moderate (i.e. in high-strength nickel-based alloys) | Moderate (i.e. commercially pure α phase titanium is very resistant; severe damages known for β-alloys)
Corrosion resistance in hot chlorides environment | Very low | Moderate to high | Moderate to high | Relatively low (i.e. to crevice corrosion and pitting)
Mechanical properties | Good | Very good | Very good | Very good
Fabricability | Very good | Good | Good | Good
Initial cost | The lowest | High | High | High to very high
Titanium – long-term
Carbon Steel – short-term
Material Selection Long-term Solutions
34
Group 4
Fusion

## Slide 35
Fusion
Group 4
Fig 23. Approximate cost of different materials relative to cost of carbon steel 2006
Source: Engineering & Technology, Fifth Edition, © 2006 Pearson Education, Inc
Fig 24. Titanium alloys cost comparison 2020
Source: www.tricormetals.com
Chart: 
| 316L | 2205 | Ti12 | Ti2 | 625 | C276 | CuNi 90-10 | Ti16 | Zr | Ti7
Price / SqFt Normalized | 16 | 47 | 71 | 78 | 123 | 141 | 249 | 401 | 462 | 616
Material Selection Long-term Solutions
35

## Slide 36
Fusion
Group 4
Reasonable
cost
Commercial
availability
Fully
α phase
High corrosion resistance in hot acids and chlorides environment
Ideal material for long-term replacement
36
Material Selection Long-term Solutions

## Slide 37
Fusion
Group 4
Titanium has superior corrosion resistance in hot chlorides and low pH environment
Different grades of titanium have been considered for the long-term replacement
Titanium grades alloyed with Palladium (Pd) and Ruthenium (Ru) have been chosen
Pd and Ru modify titanium oxide film to be less easy to dissolve
Fig 25: Crevice corrosion guideline for titanium [x]
crevice corrosion is possible here
135 (max)
Fig 26: Schematic illustration of mechanisms for high corrosion resistance in: a) Pd solid solution alloy b) micro-precipitates type
a)
b)
Material Selection Long-term Solutions
37

## Slide 38
Fig 28: Relative cost of various titanium grades
Fig 27: Pd- and Ru-doped titanium alloys: common names vs ASTM Grades
Material Selection Long-term Solutions
38
Group 4
Fusion

## Slide 39
Group 4
Titanium Grade 7
Titanium Grade 11
Titanium Grade 16
Titanium Grade 26
Commercially available
Pure α grade
Similar corrosion resistance to Ti Gr. 7
Relatively low cost
Equivalent mechanical properties to Ti Gr. 7
Doped with
0.1 wt% Ru
Relatively low cost
Commercially available
Pure α grade
Similar corrosion resistance to Ti Gr. 7
Relatively low cost
Equivalent mechanical properties to Ti Gr. 7
Doped with
0.05 wt% Pd
Relatively low cost
Commercially available
Pure α grade
Most corrosion resistant Ti alloy
Relatively high cost
Commercially available
Pure α grade
Most corrosion resistant Ti alloy
Relatively high cost
Excellent weldability and fabricability
Excellent weldability
0.15 wt% Pd
0.15 wt% Pd
Most corrosion resistant Ti alloy
Most corrosion resistant Ti alloy
Low strength
Moderate strength
Low strength
Low strength
Material Selection Long-term Solutions
39
Group 4
Fusion

## Slide 40: Conclusions
Fusion
Group 4
40

## Slide 41
Fusion
Group 4
MEG returns onshore with contaminants, mainly salts
Salts are removed by vacuum distillation so it can be recycled
Possibility that organic acids are present under normal operations
Primary material of construction is Ti Grade 12
The root cause is the oxygen ingress which occurred at evaporator
Resulted in an accumulation of organic acids
This imposed corrosion mechanisms which result metal dissolution and embrittlement (crevice corrosion & cracking)
Defects occurred where they did due to microstructure changes as a result from welding
Consequences are high and so is the probability
Mitigation methods are to minimize oxygen ingress, carry out effective inspections, plan emergency repairs and implement a robust long-term plan
Alternative material include carbon steel for emergency repairs, Titanium Grade 7 or 11 for longer term more durable repair
Lessons Learned
Add redundancy to the system
Improve personnel training and awareness
Increase capacity of the plant and make the glycol intake continuous via a pipeline
Improve corrosion risk assessment
41
Conclusion

## Slide 42
Thank you for your attention
Group 4
42
Fusion

## Slide 43
Fusion
Group 4
43
References
[1] Cramer S. D., Covino B. S. Jr., Stephen D., 2005: ASM Metals Handbook Volume 13B, Corrosion: Materials
[2] Roberge P.: Handbook of Corrosion Engineering
[3] Titanium Metals Corporation, TIMET ®, 1997: Corrosion Resistance of Titanium
[4] Hall J. A., Banerjee D., Wardlaw T. L., 1984: Titanium Science and Technology Proc., 5th International Conference on Titanium: The relationships of structure and corrosion behaviour of Ti-0.3Mo-0.8Ni (TiCode-12)
[5] Titanium Welding Course “Soudabilite du Titane et de ses Alliages” – Institut de Soudure
[6] TWI Website: https://www.twi-global.com/technical-knowledge/job-knowledge/
[7] API 5L - Forty-sixth Edition, April 2018 – Line Pipe
[8] ASME B31.3 2018 - Process Piping
[9] ASME B16.5 2017 - Pipe Flanges and Flanged Fittings: NPS 1/2 through NPS 24 Metric/Inch Standard
[10] G. W. Wille, J.W., 1981 – Hydrogen in Titanium Alloys
[11] Thomas R., TIMET ®, 2003: Titanium in Geothermal Industry
[12] Engineering & Technology, Fifth Edition, © 2006 Pearson Education, Inc

## Slide 44
Fusion
Group 4
Contamination O, H, N
from air
Poor gas shielding
Brittle structure
Contamination Fe from dust
Poor bevel cleaning, presence of dust containing iron
Preferential corrosion sites
Formation of Fe eutectic in HAZ
Titanium is very reactive with O, H, and N above 500⁰C
Titanium
H
O
O
N
Surface
oxyde
Contaminated zone
Welding (Appendix) Potential Contamination
44
Fig XX. Light micrograph showing a crack near the FL
Base metal
Weld metal
HAZ
Fusion line
Fig XX. Example of oxidized weld
Fig XX. Contamination process
Notes: The maximum tolerable limits in weld metal have been estimated as 0.3% oxygen, 0.15% nitrogen and 150ppm hydrogen so scrupulous cleanliness is essential for both parent metals and filler wires.

## Slide 45
Fusion
Group 4
Fig xx Effect of temperature and pH crevice corrosion of Titanium Grade 12 in saturated NaCl brine
Fig xx Crevice corrosion mechanism for titanium in aqueous chloride media
crevice
anodic site
cathodic site
salt deposit
Pitting / Crevice Corrosion (Appendix)
Crevice corrosion, next to pitting, was one of the primary degradation mechanisms
Pits developed on the salt-free surface and crevices developed under the slurry salt deposits
Because of the small, restricted volumes of solution within tight crevices pH levels as low as 0 to 1 could develop
45
135℃

## Slide 46
Fusion
Group 4
Fig X. Hydrogen embrittlement mechanism
Hydrogen was adsorbed on the surface of a metal, dissociated
Individual hydrogen atoms were absorbed and diffused through the titanium bulk.
Fig 16. Images showing the crack and the fracture face in section MetJB1.
Titanium
hydride layer
Ligament
(Titanium Grade 12)
Note: Hydrides dissolve easily in temperature above 100 to 150°C allowing hydrogen diffusion within the material [x]. Max. operating temperature stated in the Case Study was 135°C.
Hydrogen atoms within the metal gradually recombined to form hydrogen molecules or combined with titanium to form hydrides.
Pressure within the metal increased leading to cracking.
Hydrogen Embrittlement – to appendix
46