## Slide 1: Ben Hudson - ICorr YEP Winner 2024 Case Study: Investigation of Dump Condenser Failures Manchester University, 19th February 2025

## Slide 2: Agenda
Introduction
Case Study and Initial Findings
Investigation and Research
Mitigation Strategies
Risk Management
Summary
Q&A

## Slide 3: Introduction
About me, the team and how we investigated a real-world problem
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 4: Introduction – About Me
Graduated in Mechanical Engineering from University of Leicester 2022 (MEng Hons)
“Mechanical & CP Engineer” at Premtech Ltd for 2+ years.
Premtech Ltd is a primary designer in the Gas Industry, undertaking a range at projects across the National Transmission System (NTS)
CP Technician Lvl 2 BS EN ISO 15257:2017
Notes: Perspective and self awareness that this project is very complex

## Slide 5: Introduction – Team 1
Team 1 – Ali Morshed (Mentor)
Álvaro González Fuentes Corrosion
Amy Johnstone Structural
Ben Hudson Mechanical
Kishan Nittur Ramesh Integrity
Notes: Perspective and self awareness that this project is very complex

## Slide 6: Introduction – Project Management
Weekly meetings on MS Teams
Monthly mentor catchups
Meeting of Minutes
Request for Information (RFI)
Gannt Charts
SharePoint
Honesty
Notes: Perspective and self awareness that this project is very complex

## Slide 7: Case Study and Initial Findings
How do you find out why something breaks?
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 8: What is a Dump Condenser?
Specialized heat exchanger used in power plants and industrial processes
Rapidly condenses large volumes of steam during sudden pressure fluctuations
Primarily used during start up and shut down procedures
Notes: Perspective and self awareness that this project is very complex

## Slide 9: Dump Condenser Failure Scenarios
Operational Information:
Two-shifting operation, shutdown every 16 hours.
Large thermal cycling (~530°C - ~150°C)
Vibration upon quenching by ~20°C feed water.
Alloy composition: C, Mn, Si, Cr, Ni, Mo, N, Ti
Intergranular cracking at Surface [2]
Reported Failure Information:
EDX Analysis – Material Composition
Fracture Surface: Zn, Al, S, Mo, Cl, Ti, Cr, Fe, Ni
Additional Elements at Fracture Surface: Zn, Al, S, Cl, Fe
Transgranular Cracking at 3mm from Surface [2]
SEM Analysis
Notes: Perspective and self awareness that this project is very complex

## Slide 10: Failure Outcomes
Dump Condensers Failure Outcomes
Safety
Efficiency
Capacity
Heat Recovery
Environmental Impacts
Cost Savings
Plant Cycling
Resource Conservation
Recognise this small crack can lead to devastating impacts
Identify how this happened and how to prevent this going forward as a Corrosion Engineer
Notes: Perspective and self awareness that this project is very complex

## Slide 11: Investigation and Research
How we determined the root cause of the dump condenser failures
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 12: Crack Initiation & Propagation
Damage Mechanism | Operating Conditions (Temperature / Process) | Affected Materials / Alloy Composition | Damage Morphology
Temper Embrittlement |  |  | 
Chloride Stress Corrosion Cracking |  |  | 
Thermal Shock |  |  | 
Liquid Metal Embrittlement |  |  | 
Vibration-Induced Fatigue |  |  | 
Notes: Perspective and self awareness that this project is very complex

## Slide 13: Damage Failure Analysis
Thermal Shock / Fatigue
Thermal Cycling
High & non uniform stress development
Intergranular crack at surface & transgranular crack propagation
Liquid Metal Embrittlement
Low melting point metal contacts specific alloys
Intergranular cracks filled with low melting metals.
Tensile stress – crack propagation
Vibration-Induced Fatigue
Dynamic loading – vibration
Cracking at stress points, discontinuity
Lack of supports / stiffening
Notes: Perspective and self awareness that this project is very complex

## Slide 14: Root Causes
Corrosion Engineering – Process, Foreign materials
Material Selection & Design
Manufacturing, Maintenance & Handling
Risk-Based Inspection
Root Causes
Notes: Perspective and self awareness that this project is very complex

## Slide 15: Mitigation Strategies
How can we collectively determine the underlying factors contributing to crack initiation and propagation? What are the short-term and long-term considerations
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 16: Crack Initiation
Mitigation | Short-term | Long-term | Feasibility
Removal of zinc source |  |  | 
Coating or sleeve for the condenser surface |  |  | 
Cleaning of the steel surface |  |  | 
Upgrade steel alloy in condensers |  |  | 
Modify temperature of steam water (Corrosion Control Matrices) |  |  | 
New condenser design to reduce thermal shock |  |  | 
Reduce turbine load |  |  | 
Notes: Perspective and self awareness that this project is very complex

## Slide 17: Crack Propagation
Mitigation | Short-term | Long-term | Feasibility
Increased surveillance using risk approach |  |  | 
Grinding and weld repair cracks |  |  | 
Change in operation conditions (Corrosion Control Matrices) |  |  | 
Reduce vibrations in the condenser |  |  | 
New condenser design |  |  | 
Replace valve like-for-like |  |  | 
Notes: Perspective and self awareness that this project is very complex

## Slide 18: Short-Term Mitigations
Liquid Metal Embrittlement
Reduced temperature gradient
General Maintenance
Reduce vibrations in condenser
Eliminate source of zinc
Thermal Shock
Increased surveillance
Vibration-Induced Fatigue
Clean to remove contamination
Failure risk assessment
Add temporary supports
Adjust operating parameters
TIME AND COST
LOW
HIGH
Notes: Perspective and self awareness that this project is very complex

## Slide 19: Long-Term Mitigations
Original design
New Design
Alternative Materials
Control System Upgrades
Double Walled Head
Increased Damping at Supports
Notes: Perspective and self awareness that this project is very complex

## Slide 20: Risk Management
Assess and mitigate the potential consequences of dump condenser failures
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 21: Risk Matrix
Severity | F | Catastrophic | Medium | High | Very High | Very High | Very High | Very High
 | E | Major | Medium | Medium | High | Very High | Very High | Very High
 | D | Severe | Low | Medium | Medium | High | Very High | Very High
 | C | Significant | Low | Low | Low | Medium | High | High
 | B | Minor | Low | Low | Low | Low | Medium | Medium
 | A | Insignificant | Low | Low | Low | Low | Low | Low
 |  |  | Remote | Rare | Unlikely | Possible | Probable | Frequent
 |  |  | 1 | 2 | 3 | 4 | 5 | 6
 |  |  | Likelihood |  |  |  |  | 
Notes: Perspective and self awareness that this project is very complex

## Slide 22: Failure Modes & Effects Analysis
Cracking of dump condenser heads
Overheating and overpressure
Fragmentation
Blockage of pipework with debris
Impact to inside of pipework
HP steam enters LP pipework
Inefficient operation
Overheating and overpressure
Trip
Failure of pipework
HP steam release
Fire or explosion
Burns and damaged pipework
Trip
Notes: Perspective and self awareness that this project is very complex

## Slide 23: Risk Assessment
Component | Failure Mode | Effect | Likelihood | Severity | Risk | Component Failure Mode Risk
Cracks identified / not inspected | LME and subsequent fatigue cracking | Inefficient operation | 5 | B | M | Very High
 |  | Trip | 4 | B | L | 
 |  | Burns & Pipework Damage | 3 | D | M | 
 |  | Fire / Explosion | 3 | F | VH | 
Inspected, no cracks identified / Short-term mitigations in place | LME and subsequent fatigue cracking | Inefficient operation | 4 | B | L | High
 |  | Trip | 3 | B | L | 
 |  | Burns & Pipework Damage | 2 | D | M | 
 |  | Fire / Explosion | 2 | F | H | 
Long-term mitigations in place | LME and subsequent fatigue cracking | Not Credible |  |  |  | N/A
Notes: Perspective and self awareness that this project is very complex

## Slide 24: Summary
Key findings, recommendations and takeaways from the YEP
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex

## Slide 25: Key Findings
Failure of Dump Condenser Heads
Liquid Zinc Embrittlement and Thermal Shock
Thermal & Vibration-Induced Fatigue
Failure Investigation
Fitness For Service Assessments
Alternative Materials
Short-Term Mitigations
Risk-Based Strategy
Long-Term Upgrades
LEARNING AND UNDERSTANDING
Notes: Perspective and self awareness that this project is very complex

## Slide 26: Recommendations and Takeaways
Meet with your team regularly
Understand your teams' strengths and identify any challenges
Manage the project together and share responsibilities
Consider anything and everything
Ask lots of questions within your team
Learning and Understanding
Notes: Perspective and self awareness that this project is very complex

## Slide 27: Q&A
Thank you for listening!
1
2
3
4
5
6
7
Notes: Perspective and self awareness that this project is very complex